## Slide 1
A new class of lignin monomers
del Rio, J. C. et al. “Hydroxystilbenes are monomers in palm fruit endocarp lignins.” Plant Physiology 174, 2072-2082 (2017) [DOI: 10.1104/pp.17.00362].
Objective Recent studies indicate that lignification is a flexible mechanism and that plants are capable of using a variety of phenolic compounds for the formation of lignin polymers. In this study, we report the occurrence of a new class of polyphenolic compounds, hydroxystilbenes, in the lignins of palm fruit endocarps.
Approach
Conduct structural analyses using lignins isolated from palm fruit endocarps – including derivatization followed by reductive cleavage (DFRC) degradation and nuclear magnetic resonance (NMR) spectroscopy – to release and identify new lignin compounds, and to determine mechanisms of incorporation into growing lignin polymers.
Results/Impacts
Hydroxystilbenes (piceatannol, isorhapontigenin, and resveratrol) were identified from isolated palm lignins by DFRC. NMR spectroscopy provided evidence that the most abundant of these, piceatannol, can cross-couple with monolignols and the growing lignin polymer to be integrally incorporated into the racemic lignin polymer.
The incorporation of nonconventional monomers, not usually present in the lignins of other plants, can open up new ways to design and engineer the lignin structure to produce polymers and plant-based biomaterials with altered properties.
BRC Science Highlight
GLBRC August 2017
Notes: Notes:
text
Title again:
Text 1-2 sentence summary?